How to print with PVA

PVA (polyvinyl alcohol) is a water soluble material mainly used to print support material. It adheres well to PLA and ABS and dissolves in hot water in a number of hours, leaving behind exceptionally clean overhangs. It will extrude well through either a standard greg's wade style extruder or a flexystruder, and tends to ooze badly. It sticks well to painters tape, and less well to PET. We recommend putting a few strips of painters tape down and printing with 2-3 layers of raft if you're using PVA as a support material.

Pros:
- Great for interior cavities and intricate parts that make removing support by hand difficult
- Leaves no residue on the bottom surface of the part
- Is mildly flexible at room temperature, making support material removal a bit easier
- Can print with embedded fibers (think laywoo-d3) and then dissolved, making it an interesting material for 3D printed tissue scaffolds.
- Sticks well to painters tape
Cons:
- dissolves in water (not suitable for most parts)
- Must be stored with a drying agent, since it will absorb moisture out of the air
Print Settings:
Printing with PVA is similar to printing with PLA, though it tends to ooze quite a bit more. Print as you would with ABS or PLA but with retraction of at least 5mm. Bump up the perimeter extrusion rate to 150% to get a small amount of interference between the part and the support.

Nozzle Temperature:	170-200 C (190 default)
Bed Temperature:	60-100 C (85 default)
Nozzle sizes:	.25-1.5mm

Sample Configuration:
; generated by Slic3r 1.0.0RC1

; layer_height = 0.4
; perimeters = 4
; top_solid_layers = 3
; bottom_solid_layers = 3
; fill_density = .2
; perimeter_speed = 90
; infill_speed = 50
; travel_speed = 130
; nozzle_diameter = 0.5
; filament_diameter = 2.89
; extrusion_multiplier = 1
; perimeters extrusion width = 0.50mm
; infill extrusion width = 0.60mm
; solid infill extrusion width = 0.53mm
; top infill extrusion width = 0.53mm
; support material extrusion width = 150%
; first layer extrusion width = 0.70mm