LulzBot Filament Testing Report

Manufacturer:	MakerGeeks
Filament Name:	HIPS
Filament Type:	HIPS
Tested By:	Brent M
Date:	01/12/2016

Ease of use:	X/10
Appearance:	X/10
Color consistency:	10/10
Print temperature Range (C):	190-230/50-60
Variance in diameter: (X.XX-X-XX)
Minimum bend radius:
Prints using current Lulzbot profiles/temps: Yes, profiles had to be created for this material

General Notes:
- Great density and feel, especially when polished
- Needed to be printed at a hotter temperature that manufacturer recommends (230 vs 190-210C)
- Color was very consistent throughout the roll.
- Nice professional looking packaging.
- The material is pretty brittle when printed (similar to laybrick), but it feeds off of the spool very nicely.
- Material tends to build up on the tip of the nozzle and cause print defects
Health/Toxicity Risks:

Ingestion
Single dose oral LD50 has not been determined.
Typical for this family of materials. Estimated LD50, Rat > 5,000 mg/kg
Skin Absorption
The dermal LD50 has not been determined.
Typical for this family of materials. Estimated LD50, Rabbit > 2,000 mg/kg
Inhalation
The LC50 has not been determined.
Repeated Dose Toxicity
Based on available data, repeated exposures are not anticipated to cause significant	adverse effects.

Environmental Risks:

Movement & Partitioning
No bioconcentration of the polymeric component is expected because of its high	molecular weight. In the terrestrial environment, material is expected to remain in the	soil. In the aquatic environment, material will sink and remain in the sediment.
Persistence and Degradability
This water-insoluble polymeric solid is expected to be inert in the environment. Surface
photodegradation is expected with exposure to sunlight. No appreciable biodegradation	is expected.
ECOTOXICITY
Not expected to be acutely toxic, but material in pellet or bead form may mechanically	cause adverse effects if ingested by waterfowl or aquatic life.

Disposal Options:

DO NOT DUMP INTO ANY SEWERS, ON THE GROUND, OR INTO ANY BODY OF WATER. All
disposal practices must be in compliance with all Federal, State/Provincial and local laws and
regulations. Regulations may vary in different locations. Waste characterizations and compliance with
applicable laws are the responsibility solely of the waste generator. The preferred options include sending to a licensed, permitted: Recycler, Reclaimer, Incinerator or other thermal destruction device.

Recommendation: