Lulzbot Filament Testing Report
Manufacturer: Owens Corning
Filament Type: PA6 - Xstrand – Glass Filled Nylon
Colors Tested: Black
Tested By: Angie Suiter
Date Started: 9/20/18
Date Completed: N/A

Printer Data
Bed Surface/Covering: Glue Stick On Sanded PEI
Toolhead Types Used: Macro – 0.8mm Nozzle
Printer Type: Mini 2
Wiper Pad Type: x2 Coated ABS Wiper Pad
Other Notes: N/A

Manufacturer Recommended Settings
Print Temp: 220-280C
Bed Temp: 80-110C
Fan Speeds: N/A
Printing Speeds: 30-100mm/s
Other: Nozzle Diameter= > 0.4mm

Pre-Printing Filament Assessment
Basic Use Research:
- http://www.aimprocessing.com/blog/considerations-for-using-glass-filled-nylon-in-small-plastic-parts-manufacturing
- https://www.sculpteo.com/blog/2017/04/26/welcoming-glass-filled-nylon-new-material-available-for-3d-printing/
- https://robo3d.com/blogs/news/3d-printing-with-high-strength-fiberglass-nylon-by-owens-corning
- https://www.forecast3d.com/wp-content/uploads/2018/06/SLS-Nylon-GF.pdf
- https://www.materialise.com/en/manufacturing/materials/pa-gf
- http://www.matweb.com/search/datasheettext.aspx matguid=eb0a8c6c5333415c8e2a2d772005ddcc
- https://www.ptonline.com/columns/is-it-glass-filled-or-glass-reinforced
- https://www.ncbi.nlm.nih.gov/pmc/articles/PMC5448969/
-

Health or Environment Risk:
7.1 - During use and thermal treatment of the product, low amounts of volatile hydrocarbons	and amino derivatives may be released. Ensure sufficient ventilation. A local extraction at	emission point may be necessary. Avoid inhalation of extrusion fumes. In case of insufficient	ventilation, wear suitable respiratory equipment. Take precautionary measures against stactic	discharges.

Disposal Options: TBD
Other SDS Notes: ---
Packaging Notes: Plastic packaging. *Spool Reels crack when baked, not good for users who need to dry their filament before use.
Minimum Bend Radius: None, snaps when bent.
Bend Test Notes: Material is too strong and brittle to register a bend, it just cracks when stressed at a finner curve that the original reel that it was molded to.
Bubble/Debris Test Results: No debris or voids
Color Consistency: No variance noticeable
Filament Diameter Variance: 0.1 mm of variance
Data Points: 2.80, 2.80, 2.80, 2.70, 2.77, 2.79, 2.80, 2.79, 2.78, 2.77, 2.77, 2.74, 2.77, 2.71, 2.73
Average: 2.768
Moisture Absorption:
Dry Measurements:
Length: N/A
Average Diameter: N/A
Weight: 0.0555 kg
Date: 10/23/2018
Time: AM
Day 1:
Environmental Humidity Level: 25-28% RH
Average Diameter: N/A
Weight: 0.0545 kg
Date: 10/24/2018
Time: AM
Day 2:
Environmental Humidity Level: 21-23% RH
Average Diameter: N/A
Weight: 0.0545 kg
Date: 10/25/2018
Time: PM
Day 3:
Environmental Humidity Level: 20-21% RH
Average Diameter: N/A
Weight: 0.0545 kg
Date: 10/26/2018
Time: PM
Day 4:
Environmental Humidity Level: ~20% RH
Average Diameter: NA
Weight: 0.0545 kg
Date: 10/27/2018
Time: PM
Day 5:
Environmental Humidity Level: ~72% RH
Average Diameter: NA
Weight: 0.0550 kg
Date: 10/30/2018
Time: AM
Humidity increase to ~83.5% RH (exposed for ~2 days)
Weight: 0.0555 kg
Humidity increase to ~83.5% RH
Weight: 0.0555 kg
Humidity increase to ~90% RH (exposed for ~3 days)
Weight: 0.0560 kg

2ND WEIGHT TEST FOR MOISTURE:

New Reel weight at open: 0.74885 kg

New Reel after Bake at 158 for ~44 hrs: 0.73920 - 0.73930 kg

Difference of ~ 0.00965 – 0.00955 kg

Min Extrusion Temp: 210
Max Extrusion Temp Before Boil: 290 (max for machine)
Min Bed Sticking Temp: 50 (75 or above recommended with PEI)
Other Notes:

Run a Control Print with an Available Comparable Material Profile
Results: N/A
Profile Used: N/A
** Material too different from previous materials, I have chosen to begin with a newly created profile as a control instead **

Recommended Profile Changes

Printing Filament Assessment
Bed Adhesion Notes: Needs a little squish to begin a stick to the bed, I recommend using light glue stick on PEI
Layer Adhesion Notes: Layers adhere better when all warmed and cooled together (post baking/bed fully cooled)
Overhang/Bridging Notes: overhang to 60* without error (some wobble if fan not strong enough)
Color Consistency/Change: No change after print, texture is a fine gritty after extruded (same as unprinted)
Part Removal Notes: part removes well with a sharp tap to the base with a spatula
Other Notes:

Profile Assessment and Base Setting Recommendations
Bed Temperature Range: 80-100C
Printing Temperature Range: 250-270C
Fan/Cooling Range: low but not off
Printing Speeds: 10-50 mm/s
Other Notes: Use Gluestick for bed adhesion ease

Manufacturer Filament Revision Notes
Revision Reason:
Expected Change:
Date: