LulzBot Filament Testing Report

Manufacturer: Village Plastics
Filament Type: PVA
Tested By: BJB
Date:	8/23/17

Ease of use:	NA/10
Appearance:	10/10
Color consistency:	10/10
Print temperature Range (C):	(185-200)
Variance in diameter: (2.85-2.90)
Minimum bend radius: NA
Prints using current Lulzbot profiles/temps: NA

General Notes:	(Be as detailed as possible)
- Filament would not extrude well at 200C. I could not exceed 200C because the SDS calls for breakdown at this temperature

Recommended Print Profiles:

Health or environmental risks:

Disposal Options:

NA

Recommendation: NA

Revision History

Revision Date	Modifications or Additions	Updated By
8/23/17	Create initial report	BJB