LulzBot Filament Testing Report

Manufacturer: Village Plastics
Filament Type: Hips 2
Tested By: Angelica Nolen
Date: 10/31/2017

Ease of use: 8/10
Appearance: 9/10
Color consistency: Filament: clear cloudy white; Printed: cool toned white/clear extrusion – UPDATE: PRINT PRODUCT YELLOWS WITH AGE (*the filament on the reel does not appear to change color over time, the printed result changes with the age of the filament being used to print with, the change is not seen until after the model has been printed with the older filament)
Print Temperature Range (C):
Variance in diameter: 0.03 mm variance (max)
Minimum bend radius: no minimum
Current Lulzbot profiles/temps Used for Tests:
Village Plastics – Hips (old profile)
General Notes:
- Packaging: vacuum sealed in clear plastic, non resealable
- Bed temp increase for adhesion (100-110 C)
- No filament inconsistencies or debris found
- When stressed, the clear cloudy color becomes flat opaque white
- MSDS noted melting point 105-135C
- Good bed adhesion, sticks a bit strong after cooling, harder to remove
- D-limonene results:
- **INCONSISTENT PRINT COLOR OVER TIME – Opened reel used and left in room temperature storage container for 3 months, no abnormal humidity or light exposure during this time.
Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)
All profile levels recommended: High Speed, High Detail, and Standard
Health or environmental risks:
- Do not inhale dust of this product or ingest
- Flashpoint: > 280 C
- keep dust from this product away from an open flame
- Keep out of soil an bodies of water (and drains?)
Disposal Options:
With due observation of the regulations laid down by the local authorities, this must be brought to a suitable incineration plant/waste disposal site.
Recommendation:
REJECTED – Inconsistent Print Color with Age

Revision History

Revision Date	Modifications or Additions	Updated By
11/07/17	Data	A. Nolen
3/02/2018	Confirm test profiles and quality	A. Suiter