Lulzbot Filament Testing Report
Manufacturer: Colorfabb
Filament Type: PA-CF (Polyamide-carbon fiber)
Colors Tested: Black
Tested By: Angelica Suiter
Date Started: 9/20/18
Date Completed: 11/13/2018

Printer Data
Bed Surface/Covering: Heated bed with PEI
Toolhead Types Used: Macro – 0.8mm Nozzle
Printer Type: Mini 2
Wiper Pad Type: x2 Coated ABS Wiper Pad
Other Notes: N/A

Manufacturer Recommended Settings
Print Temp: 260 – 280 C
Bed Temp: Cold if low infill, 40 – 50 C if high infill
Fan Speeds: 50%
Printing Speeds: 30 – 40 mm/sec
Other: (bed – buildTak, Glass Plate)

Pre-Printing Filament Assessment
Basic Use Research:
- https://www.sciencedirect.com/science/article/pii/S135983681300125X
- https://www.sciencedirect.com/science/article/pii/S0266353803001192
- http://www.sohim.by/eng/production/carbon/plastics/
- http://www.madehow.com/Volume-4/Carbon-Fiber.html

Health or Environment Risk:
7.1 - Handling and Storage:
Provide for appropriate exhaust ventilation at machine. Do not breath
vapours/dust. Wear personal protective equipment.
The material can accumulate static charge and can therefore cause
electrical ignition. Take measures to prevent buildup of electrostatic
charge.
Handle in accordance with good industrial hygiene and safety practice.
Avoid contact with skin and eyes. Wash hands before breaks and
immediately after handling the product. Keep away from food and drinks.
When using, do not eat, drink, smoke.
8.2 – Exposure controls
Respiratory protection – Not required (for FDM printing);
Environmental exposure controls – Do not allow product to enter drains, water courses	or soil.
Disposal Options: In accordance with local laws.
Other SDS Notes: ---
Packaging Notes: Standard Colorfabb Packaging, plastic bag inside box, wrapped in plastic wrap
Minimum Bend Radius: None. Snaps when bent.
Bend Test Notes: Material very brittle if bent out of spooled coil shape, edges sharp when broken
Bubble/Debris Test Results: No voids or Debris found
Color Consistency: No change in color from reel to printed part or throughout printed parts, also no change on reel.
Filament Diameter Variance: 0.11 mm
Data Points: 2.80, 2.79, 2.82, 2.83, 2.87, 2.79, 2.79, 2.76, 2.84, 2.80, 2.81, 2.78, 2.79, 2.78,	2.79, 2.79, 2.81.
Average: 2.80 mm
Moisture Absorption:
Dry Measurements:
Length: N/A
Average Diameter: N/A
Weight: 0.0535 kg
Date: 10/23/2018
Time: AM
Day 1:
Environmental Humidity Level: 25-28%
Average Diameter: N/A
Weight: 0.0535 kg
Date: 10/24/2018
Time: AM
Day 2:
Environmental Humidity Level: 21-23%
Average Diameter: N/A
Weight: 0.0535 kg
Date: 10/25/2018
Time: PM
Day 3:
Environmental Humidity Level: 20-21%
Average Diameter: N/A
Weight: 0.0525 kg
Date: 10/26/2018
Time: PM
Day 4:
Environmental Humidity Level: ~20%
Average Diameter: N/A
Weight: 0.0535 kg
Date: 10/27/2018
Time: PM
Day 5:
Environmental Humidity Level: ~72%
Average Diameter: N/A
Weight: 0.0545 kg
Date: 10/30/2018
Time: AM
Humidity increase to ~83.5% RH (exposed for ~2 days)
Weight: 0.0540 kg
Humidity increase to ~85% RH
Weight: 0.0545 kg
Humidity increase to ~90% RH (exposed for ~3 days)
Weight: 0.0550 kg

Min Extrusion Temp: 240 (do not print this low, only hand fed extrusion test)
Max Extrusion Temp Before Boil: 290 C (moisture in filament?), do not print above 280 C
Min Bed Sticking Temp: 45 C
Other Notes:

Run a Control Print with an Available Comparable Material Profile
Results: N/A
Profile Used: N/A
** Material too different from previous materials, I have chosen to begin with a newly created profile as a control instead **

Recommended Profile Changes
---

Printing Filament Assessment
Bed Adhesion Notes: Sticks to PEI well, no material warp
Layer Adhesion Notes: print in an enclosure if possible, good layer adhesion with higher temp and lower fan. Let cool completely before removing from bed for best results.
Overhang/Bridging Notes: Overhangs print very well, this material wants to stick to itself. Bridging needs some fan to cool the extrusion rapidly to solidify.
Color Consistency/Change: No change in color from reel to print or throughout print.
Part Removal Notes: one sharp tap to the bottom of the part AFTER the bed and part have had time to cool fully, removes well.
Other Notes:

Profile Assessment and Base Setting Recommendations
Bed Temperature Range: 45-75 C
Printing Temperature Range: 255 – 280 C
Fan/Cooling Range: 0-30% (if part has no bridging you can turn the fan off for a higher strength)
Printing Speeds: 15-50 mm/s (Slower speeds for thicker layer heights)
Other Notes: Overall this material prints well. Parts printed with this may gain strength from a post baking process (testing ongoing), TDB.

Manufacturer Filament Revision Notes
Revision Reason:
Expected Change:
Date: