LulzBot Filament Testing Report

Manufacturer: E3D Online
Filament Type: Scaffold
Tested By:	bam
Date:	12.16.16

Ease of use:	6/10
Appearance:	8/10 (Support material, color is irrelevant)
Color consistency:	10/10
Print temperature Range (C):	(180-200/0-90)
Variance in diameter: (2.84-2.89)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps: No

Manufacturers Properties:
Melting point: 150-230ºC
Flash point: >200ºC
Decomposition Temp: >200ºC
Auto-ignition temperature: 520ºC

General Notes:

- Do NOT print at or above the decomposition temperature of 200ºC
- E3D has fixed the issues with moisture absorption causing constant clogging, unfortunately the new formulation needs to be printed at 215C in order to avoid stripping, which is well in excess of the thermal decomposition temperature.

Health or environmental risks:

Dangerous Decomposition Products: Build-up of dangerous/toxic fumes possible in cases of
fire/high temperature.

Conditions to avoid: No data available

Ecological:
Mobility: No data available
Bioaccumulation: Readily biodegradable
Ecotoxicity effects: Data not available.

Disposal Options:
Disposal: In accordance with local and national regulations. Do not dispose of together with household
waste. Waste codes should be assigned by the user based on the application for which the product was used. Recommend putting this on product page if we carry the material since it's likely to get dumped down a drain.

Recommendation: This material does not print reliably below 200C, the listed thermal decomposition temperature on the SDS. Until we can get test data and an updated SDS showing that the material is safe at 215C we cannot print this filament or recommend that our customers do.