Enye labs Filament testing notes:

Manufacturer:	Enye labs
Filament Name:	Recycled PET – clearish – 2.80mm
Filament Type:	Off-clear PET – 100% recycled
Date:	3/18/2015

Ease of use:	2/10
Appearance:	Good color – looks like what you'd expect from soda bottles
Size consistency:	Average, but a bit low
Color consistency:	Good, come black contaminants
Print temperature:	240/60 (LulzBot Mini)
Prints using Lulzbot profiles/temps: No

Notes:
b-pet
- A 100% recycled filament is something that a lot of people have been waiting for, and PET is probably the best material to do it with.
- The color is a bit off of clear, with some brown and green added in. I'm not sure if this will deter customers, but I think it's almost a feature -it's just about the color you'd expect from melted down soda bottles.
- Filament size consistency was about on par with most filament, but nominal size was a bit low. If this is consistent we can compensate for it in the filament profile, but it didn't cause any issues in the test prints we ran.
- This filament has a very narrow print temperature range between being able to extrude at all (230) to where it starts to boil (245). That being said, it printed mostly consistently once we got the temperature right.
- It should be fairly cheap compared to other PET's. The filament manufacturer has it on their website for $30/kg, compared to 66$/kg for t-glase and 163$/kg for the chipped “ekocycle” filament from 3D Systems.
- The sample rolls received contained lots of contaminants
Recommendation: .

This stuff is great, but not quite there yet. It is more finicky to print with than t-glase, but with a lower pricepoint and 100% recycled content I think a lot of people would prefer it if the contamination could be dealt with.

Filament diameter accuracy / consistency:

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
b-pet	2.70-2.82 (.12mm)	0.06mm (2.76-2.82)	230-240C (printed at 235C with .5mm hex nozzle)