E-sun filament testing notes

Red 3mm ABS:
- Diameter varied in a random 1m sample from 2.81 to 2.91mm
- Oozes a bit at 230C, not worse than Village plastic's red ABS

Orange 3mm ABS:
- Diameter varied between 2.78mm and 2.91 over the 3M sample
- Prints well at 230C
- Parts seem more brittle than Village ABS, more like HIPS

3mm natural PVA:
- Boils out of extruder at above 200C, coats inside of buda badly
- Prints well @ 190C
- Dissolves in cold water overnight, much faster in warm moving water (washing)
- Adheres well to ABS printing at 200 (PVA) and 230 (ABS)
- Diameter varied from 2.65 to 2.93mm

3mm HIPS (yellow)
- Prints similarly to ABS
- Diameter of filament sample ranged from 2.82-2.95mm
- Still warped a small amount, but better than ABS
- Has a nice dry look and feel

3mm Natural PLA
- Prints easily at 170-195, oozes quite a bit
- VERY similar to Village PLA
- Diameter was pretty consistent (2.76-2.85mm)
- Back of octopuses’ head warped, would probably do better with a fan

3mm Conductive ABS
- Prints very similar to regular abs.
- Doesn't stick to the PET bed as well as normal abs.

Conductive ABS