LulzBot Filament Testing Report

Manufacturer: IC3D
Filament Type: PA 747 ABS
Tested By:	Baldwin
Date:	11/30/16

Ease of use:	7/10
Appearance:	10/10
Color consistency:	10/10
Melting Temperature Softening: < 100˚C
Print temperature Range (C):	(220ºC-260ºC)
Variance in diameter: (2.77-2.89)
Minimum bend radius: N/A (r < 3mm)
Prints using current Lulzbot profiles/temps:
Village Plastics ABS profiles work pretty well at lower bed temps ~90-95C

General Notes:	(Be as detailed as possible)
- Glue is not necessary
- Thermal Decomposition Temperature in air 270˚ C
- Do not exceed Thermal Decomposition Temperature
- Seems to be slightly more brittle than other ABS
- Very sticky on PEI at 110C
- Just about the right stickiness at 90-95C

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)
TAZ and Mini profiles include high speed, medium quality, high detail.

Health or environmental risks:

Thermal Decomposition Gases CO, HCN, AN, SM and NO

Disposal Options:

To avoid being taken by ocean species or birds, disposal of the waste to the ocean and
water sources is inhibited.
Controlled incineration or landfill according to local, state or national laws and
regulations concerning health and pollution.
Inadequate incineration may generate toxic gases such as CO, HCN, AN and SM.

Recommendation:	(As thorough as possible)

Overall, this filament isn’t bad. The only real problem is that it is very sticky. I did have some real trouble removing parts from the PEI at 110C. This could pose a real issue for new less experienced users (high potential for bed damage on removal). However at 90-95C the part stuck well but not too well. ( could potentially save heat beds.)The finish of the material is nice and is a consistent thickness.
I’ve better luck with strength extruding at a lower temp (235C). I have encountered some difficulty running low layer height prints, however it excels at standard to high layer heights. In my opinion this ABS is a great choice for prints that would normally call for a quality ABS.

Revision History

Revision Date	Modifications or Additions	Updated By