LulzBot Filament Testing Report

Manufacturer: Polymaker
Filament Type:	SU301 (PVA)
Tested By:	D. Hall
Date:	8/23/17

Ease of use:	7/10	7( possible brittle issue) Initial opening, cannot bend well. After one week of testing, no breaking of the filament in the guide tube, or breaking while printing. Overall not too brittle,.

Appearance:	10/10

Color consistency:	10/10

Print temperature Range (C):	Recommended 210-220C, using 190C to start, will increase at intervals

Variance in diameter: (2.81 – 2.90

Minimum bend radius: Cannot bend past approximately 70 degrees without snapping the filament. Have been able to bend to 90 degrees on occasion, but not repeatable.
Filament “brittleness”: as of 8/29/17, filament is no more brittle than one week ago. No “strip outs” as of yet.
After one week of testing, no breaking of the filament in the guide tube, or breaking while printing. Overall not too brittle,.

Prints using current Lulzbot profiles/temps:
1. Dolphin stl. 190 C with 160 C standby temp
2. Arch triumph stl. 210C with 170C stanby temp. note:( standby works better at 160C)
2 successful tests, different sizes.
3. 1 unsuccessful Dolphin print, due to a settings issue, not a filament issue.
4. Iguana stl. 210C with 170C standby temp. “spiralize” on. Successful, but do not recommend “spiralize”

General Notes:	(Be as detailed as possible)

V3 Dually used on testing
- Using glue stick. No information available. Will try without glue stick .
- Good adhesion, fluid layering,
- NO Seeping! (@190)
- Wipe tower operates well (Cura2) no residual filament from seeping.
- Good quality on color
- Prints well at210C with a little more “seeping”, but without deforming the print.

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Health or environmental risks:
See SDS for information.
Nothing noted.

Disposal Options:

Recommendation:	Use standard PVA settings, with a temperature change.
Successful prints at 190, 205 and 210C. 210C appears to get the best layering and attachment to the PLA that I am testing with.
All tests have been successful, with no stripping and no fails to this point.

Filament disolving:
1. Starting testing, first application: 24 oz. Water and 1 meter of filament. No agitation. Took 5 hours to dissolve.

2. Test with 24 oz. Water and 1 meter of filament. Agitate the bin once every ½ hour. Took 5 hours to dissolve.
No difference in time. Suspect that constantly moving water will be the only thing that will make the filament dissolve more rapidly.

Revision History

Revision Date	Modifications or Additions	Updated By