Recreus FilaFlex Filament testing notes:

Notes:
Brown Filaflex
- This stuff is far more consistent in diameter than the last samples I tested from them, but still has much more variance than Ninjaflex or any of our rigid filaments
- Feels much more flexible than ninjaflex
- They've perfectly matched the color of dog poop
Black 3mm Filaflex
- This is about as consistent as the brown 3mm filaflex; it's way better than filaflex used to be but still pretty bad compared to most of the other filaments on the market today
- Strings badly at 230, prints much better at 220 but speeds need to be reduced
Recommendation: .

They're getting better at extruding the stuff, but it's still not there yet. I think the only reason to have this in the store is if we can get it as a cheaper alternative to the generally better ninjaflex. It comes in some nice colors but the inconsistency in diameter makes it a worse alternative to ninjaflex.

Filament diameter accuracy / consistency:

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
Brown 3mm	2.63-2.88 (.25mm) / ninjaflex typically varries from 2.84 to 2.91 for reference	0.09mm (2.71-2.80)	225-230C, very stringy at 230, stripped at 220. Most likely needs to be printed at ~220 at lower speeds than ninjaflex
Black 3mm	2.61-2.85 (.24mm)	0.08mm (2.67-2.75)	Printed same as brown filaflex
Average	2.74mm (+/- 0.15mm)	0.085mm (Not great)