LulzBot Filament Testing Report

Manufacturer:	Toner Plastics
Filament Name:	2.88mm TPU, Lot# 41420
Filament Type:	Clear TPU
Date:	2/11/2015

Ease of use:	6/10
Appearance:	Great, looks like T-glase when printed
Size consistency:	Excellent (for TPU)
Color consistency:	No variance
Print temperature:	230/50 (LulzBot Flexystruder)
Prints using Lulzbot profiles/temps: Yes

Recommendation: This stuff prints just like our current TPU, ninjaflex. It might not make sense to carry it alongside ninjaflex if it only comes in clear, but if they can get more colors out it could be a great alternative.

Notes:
- This stuff prints well in the flexystruder, almost exactly the same as ninjaflex
- This stuff definitely needs the flexystruder
- It also looks about the same as ninjaflex when printed, but several people were crazy about how clear it is before printing.
- The smooth surface doesn't seem to have much effect when compared to ninjaflex

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
2.88mm TPU	2.88-2.93 (.05mm) / Note: This is AWESOME for an elastomer	0.03mm (2.88-2.91)	210-240C (printed at 230C with standard flexystruder)