LulzBot Filament Testing Report

Manufacturer: Toner Plastics
Filament Type: HIPS
Tested By:
Date:

Ease of use:	X/10
Appearance:	X/10
Color consistency:	X/10
Print temperature Range (C):	XXX-XXX/XX-XX
Variance in diameter: (X.XX-X-XX)
Minimum bend radius:
Prints using current Lulzbot profiles/temps:

Manufacturers Temperatures: Melting point: >120°C

General Notes:
- Great density and feel, especially when polished
- Needed to be printed at a hotter temperature that manufacturer recommends (230 vs 190-210C)
- Color was very consistent throughout the roll.
- Nice professional looking packaging.
- The material is pretty brittle when printed (similar to laybrick), but it feeds off of the spool very nicely.
- Material tends to build up on the tip of the nozzle and cause print defects

Health risks:

Ventilation: Necessary for fumes and gases when melting.
Personal Protection Eyes: Wear safety glasses or chemical goggles for general purpose.
Respiratory: Wear appropriate respiratory masks as needed.
Gloves: Necessary for handling melted material.
Note: It is the responsibility of the user to determine the adequacy of any protection or safety measures.

Environmental risks:

Aquatic toxicity: No evidence of aquatic toxicity.
Mobility in soil: No data available
Persistence and degradability: Toner Plastics HIPS 3D Printer Filament
Biodegradation: Product is not readily biodegradable, the product is likely to persist in the environment.
Additional ecological information: General information: Do not allow to enter into ground-water, surface water or drains.

Disposal Options:

Controlled incineration or landfill according to local, state or national laws and regulations concerning health and pollution.

Recommendation: