LulzBot Filament Testing Report

Manufacturer: Verbatim
Filament Type: BVOH
Tested By: Ben B.
Date: 8/8/17

Ease of use:	7/10
Appearance:	7/10
Color consistency:	N/A
Print temperature Range (C): 190c-240c
Variance in diameter: 2.88mm – 2.95mm
Minimum bend radius:
Prints using current Lulzbot profiles/temps: PLA profiles, increased temps possible 195c - 225c

General Notes:	(Be as detailed as possible)
- Gluestick helps initial plate adhesion
- Initial tests show poor adhesion to Amphora type materials
- Multiple strip outs when using dual extruder v3
  - Bag open less than 24 hours for first one
  - 3 total over ~1kg
- Strings less than normal PVAs
- Higher temp range should allow compatibility with more materials
  - PLA and Nylon work well
- Some issues adhering on top of PLA
  - Strange as underside support did not exhibit same issues
  - VP PLA, PM PLA, and VPLA all exhibited same trait

Recommended Print Profiles: PLA base profile, with temp 195c - 225c good starting point

Health or environmental risks: Do not print above 240c, risk of combustion

Disposal Options: Contact local waste authorities

Recommendation:	(As thorough as possible)

BVOH can print well, while being slightly susceptible to moisture absorption. Recommend keeping in a sealed desiccant bag when not in use. 90-95% flow rate to help accommodate for die swell recommended. Strange issue of not adhering to top of PLA. Suspect profile tweaks could be a solution. Compared to all other water soluble materials we have tested, more reliable than average.

Revision History

Revision Date	Modifications or Additions	Updated By
9/13/17	Added personal testing feedback	BI